8D Problem Solving Report

Report No.: 8D-PT2024-ABS-2025-1218
Customer: Customer Assembly (SITE-A Plant)
Plant / Supplier: Sample Supplier Plant
Part Name: ABS Carrying Case
Model: PT-2024-Pro
Drawing Rev.: Rev.C (released)
Customer Complaint Date: 2025-12-18
Related Lots: #20251215, #20251216 (per customer info)
Defect Type: Hinge corner cracking during assembly
Severity: Critical functional defect; potential line stoppage; customer escalation level: L2

D1: Team Formation

Leader: Quality Engineer A Chen – Quality Engineer (8D owner)
Members:

- Production Supervisor A Wu – Molding Supervisor (Shift A/B coverage)

- Process Engineer A Zhang – Process Engineer (Injection parameters owner)

- Lab Technician A Gao – QE Lab Technician (failure analysis, testing)

- Logistics Lead A Liu – Production Planner (traceability, shipment containment)

Kick-off Meeting: 2025-12-18 14:00 (SZ time)
Customer Contact: SITE-A Quality – Customer Contact A (Complaint ID: NB-CR-251218-07)

D2: Problem Description

1) What / Where / When

- What: Crack at hinge corner, visible as hairline fracture and/or full corner split.

- Where: Part feature “Hinge Corner – Left”, near radius R0.8 transition to vertical wall (per Rev.C drawing).

- When: Found during customer site assembly step AS-07 (“Hinge pin insertion + cover closure check”), first noted on 2025-12-18.

2) Quantification (Customer Data)

- Customer inspected 500 pcs, found 25 cracked → 5.0% defect rate.

- Customer indicated suspect is Lot #20251215.

- Additional customer stock at warehouse: ~2,000 pcs pending usage.

3) Defect Criteria (Customer / Supplier alignment)

- Customer criterion: Any visible crack > 3 mm at hinge corner = reject.

- Supplier criterion: Any crack visible under 500 lux light at 30 cm distance = reject.
(Note: Criteria alignment recorded on 2025-12-19, email confirmation.)

4) Symptom Observations (SYNTHETIC)

- Crack orientation: typically 45° from corner toward hinge rib.

- Crack visibility: 70% visible by naked eye; 30% detected after light flexing of hinge area.

- Reported occurrence: concentrated in one assembly line (Line 2) per customer verbal note.

5) Impact

- Function risk: hinge stiffness fails, cover does not close flush; potential field failure.

- Customer action: temporary hold on PT-2024-Pro shipment to end users (internal hold).

D3: Interim Containment Actions (ICA)

Containment Plan Summary

| Containment Location | Scope | Method | Owner | Start | Result |
| --- | --- | --- | --- | --- | --- |
| Customer warehouse | 2,000 pcs | 100% sorting (visual + flex) | Customer + Quality Engineer A | 12/18 | 89 defective found |
| In-transit shipment | Lot #20251216 (1 shipment) | Return to supplier for sorting | Logistics Lead A | 12/18 | Shipment returned 12/19 |
| Supplier internal WIP | Machine #4 WIP & FG | Stop production + quarantine | Production Supervisor A | 12/18 | 1,200 pcs quarantined |

Sorting Work Instruction (Customer site, SYNTHETIC):

- Visual check at 500–800 lux

- Manual flex: apply ~15 N at hinge corner (operator training 10 min)

- Record by carton ID; carton label includes cavity no., date, shift code.

Traceability Extract (Supplier, SYNTHETIC):

- Lot #20251215: Machine #4, Mold M-PT-ABS-02, Cavities 1–4, Shift N (night) + Shift B (day partial).

Stop Ship Decision: All PT-2024-Pro cases from Machine #4 held until root cause confirmed.

D4: Root Cause Analysis

1) Initial Checks

- Material verification: Virgin ABS, grade “ABS-9300”; COA within spec (MFR, moisture).
Conclusion: not a material mix-up.

- Mold inspection: No visible damage on core/cavity; gate area OK; hinge feature surface OK.
Conclusion: no obvious mold damage.

- Process check (Machine #4):

  - Hold pressure recorded at 85 MPa (current)

  - Standard parameter sheet shows 70 ± 5 MPa

  - Hold time: 6.0 s (standard 5.0 s)

  - Mold temperature: 55°C (standard 50°C)

2) Evidence Collected (SYNTHETIC)

A. Weight comparison (10 pcs each group)

| Group | Condition | Avg weight (g) | Range (g) |
| --- | --- | --- | --- |
| Good reference | Lot #20251210 | 148.2 | 147.8–148.6 |
| Suspect | Lot #20251215 | 149.4 | 148.9–150.1 |

B. Simple stress indicator

- Hot water soak 60°C, 10 min: suspect group showed micro-crack initiation in 2/10 samples at hinge corner.

C. Failure replication attempt

- At 85 MPa hold pressure, hinge corner cracks observed after assembly simulation in 3/20 pcs.

3) 5-Why Analysis

- Why did the part crack at customer assembly?
→ High internal stress at hinge corner + stress concentration during pin insertion.

- Why high internal stress?
→ Over-packing during hold stage increases residual stress.

- Why over-packing?
→ Hold pressure set higher than standard (85 MPa vs 70 ± 5 MPa).

- Why was hold pressure too high?
→ Night shift technician adjusted it manually to address “short shot” symptom.

- Why was manual adjustment allowed and not detected?
→ Parameter changes not locked; shift handover checklist did not include parameter verification.

4) Root Cause Conclusion

- Occurrence root cause: Process parameter violation (hold pressure/hold time higher than standard), increasing residual stress at hinge corner.

- Escape root cause (preliminary): Lack of parameter lock + inadequate shift handover verification.

(Fishbone considered: material, mold, machine, method, man, measurement. Primary path confirmed as “method/man”).

D5: Permanent Corrective Actions (PCA)

Corrective Actions List

| No. | Action | Type | Owner | Due | Status |
| --- | --- | --- | --- | --- | --- |
| 1 | Reset Machine #4 recipe to standard (Hold pressure 70 MPa; Hold time 5.0 s; Mold temp 50°C) | Corrective | Process Engineer A | 12/19 | Done |
| 2 | Retrain night shift technician on SOP-MOLD-001 + parameter change control | Preventive | Production Supervisor A | 12/20 | Done |
| 3 | Issue warning letter to technician (policy HR-QA-07) | Disciplinary | Quality Engineer A | 12/20 | Done |
| 4 | Post “DO NOT TOUCH PARAMETERS” sign on HMI | Preventive | Production Supervisor A | 12/19 | Done |
| 5 | Add shift handover checklist item: verify recipe checksum + key parameters | Preventive | Quality Engineer A | 12/22 | In progress |
| 6 | Enable HMI password for recipe edits (Engineer only) | System | Process Engineer A | 12/28 | Planned |

Updated Standard (posted at machine):

- Hold pressure: 70 MPa

- Hold time: 5.0 s

- Injection speed: 120 mm/s

- Packing-to-hold switchover: 98%

- Cooling time: 18 s

D6: Validation of Corrective Actions

Validation Build (SYNTHETIC)

- Build date: 2025-12-20

- Machine: #4

- Quantity: 50 pcs (first-off validation)

- Conditions: standard recipe + same mold + same material grade

Tests Performed

- Assembly simulation (AS-07 equivalent): 50/50 pass, no cracks observed.

- Drop test: 1.0 m, 6 faces, 1 cycle each → 50/50 pass.

- Visual + flex screening: 0/50 defects.

Conclusion

Corrective action is validated. Production can resume under controlled parameters.

D7: Prevent Recurrence

System/Process Controls (SYNTHETIC)

- Update training matrix for injection department (all shifts).

- Add “recipe verification” into Layered Process Audit (LPA) weekly checklist.

- Update SOP-MOLD-001: include parameter change authorization requirement.

- Add Control Plan item: monitor hold pressure (target + tolerance) every 2 hours.

Effectiveness monitoring: Track cracking defects for next 3 production lots; target <0.3%.

D8: Team Recognition

Team thanked for rapid containment and resolution. Case closed on 2025-12-21.